RELATION OF  GAMMA-IRRADIATED NA-BENTONITE CLAY  MINERALOGY TO ORIGIN OF GUNASHLI PETROLEUM

I.I.Mustafayev,  M.K.Ismayilova, S.G.Mammadov, F.N.Nurmammadova

Azerbaijan National Academy of Sciences, Institute of Radiation Problems, Baku.

АZ 1143 Bаku, Azerbaijan, B.Vahabzadeh str.

E-mail: ismayilovamehpara@gmail.com

Petroleum is a product of the diagenesis of fundamental organic compounds in organic matter that accumulated with fine-grained sediment in a low-energy environment deficient in oxygen. The diagenesis takes place during burial, under the influences of heat, time and pressure – probably in the presence of clay catalysts[1].

Contempory science does not yet know any microbe which really generates n-C11 – n-C22 alkanes, phytan, pristan and aromatic hydrocarbons. In present work was studied the smectite dehydration under gamma rays  – its relation to structural development and hydrocarbon accumulation in Gunashli oilfield, Azerbaijan. Radiation – induced damage in Na-bentonite clay caused formation of arenes, cycloparaffines, branched and unsaturated hydrocarbons, namely generation of hydrocarbons from Gunashli oil field [2,3].

It was revealed that the process of destruction of silico-alumina nucleus of clay minerals is becoming more active in a particular sequence of cation out let of crystal lattice: Fe3+ > Ca2+  > Mg 2+  > Na+ > K+  > Si4+. Exept for the destruction of a solid phase of clays, there is radiolysis of pore water, which results in the formation of free radicals. The catalytic conversion of  hydrocarbons of petroleum occurring on contact with irradiated solids. The main essence of radiocatalytic processes is transferring the unbalanced charges formed by absorbed ionizing radiation energy on the surface of the catalyst to the system[3,4]. Under the effect of ionizing radiation  valence electrons(F) and hole centers(V) form in bentonite clay crystals.

The experimental results discussed in the work[5] confirm that the CaCO3 - FeO – H2O system generates the suite of hydrocarbons in characteristic of natural petroleum. Proposed catalyst sodium –bentonite clay (Alpoid deposit contains more than 85% of Na- montmorillonite -(Na,0.5Ca)0.7(Al,Mg,Fe)4(Si,Al)8O20(OH)4·XH2O)  consist of complex oxides and water. This research gives a new approach for study the metamorphism of crude oil [6].

References

- Ed.by  R.E.Chapman. Origin and Migration of Petroleum: Geological and Physical Aspects . Developments in Petroleum Science. V. 16, 1983, P. 179-207.

- M. K.Ismayilova.  Influence of energy transfer in the adsorbed state of   the clay at the petroleum radiolysis under gamma-radiation at room temperature. Radiation effects and defects in solids. 2020,V.175/5-6,pp 472-481,  DOI:10.1080/10420150.2019.1678622

- M.K.Ismayilova. Eeffects of gamma-irradiation on nanostructured Na-bentonite silicate   layers at room temperature. Problems of atomic science and technology. 2021. №5(135),        p. 51-56.

- J.Merkel,B.Planer-Friedrich,C.Wolkers-dorfer.Uranium in the aquatic environment. Germany, Springer-Verlag Berlin, Heidelberg. 2002.p.134-136.

- V.G. Kutcherov, Abiogenic deep origin of hydrocarbons and oil and gas deposits formation, (2013). DOI:10.5772/51549

- I.I.Mustafayev, M. K.Ismayilova. Review: The role of radiation, Fe(III) oxides and montmorillonite in organic metamorphism.2018. Journal of Radiation Researches. 5 (1),                p. 40-46